Data-driven rational screening of silver nanoparticles: An explainable machine learning approach for antimicrobial efficacy prediction and structure-activity-guided design

Jun-Wei Lianga, Yi-Jia Chena, Yun-Lang Fenga, Giovanna Moura Silvab, Gabriela Patrícia Unigarro Villarrealb, Leonardo Fernandes Fracetob & Wen-Hao Sua*

aCollege of Engineering, China Agricultural University, 17 Qinghua East Road, Haidian, Beijing 100083, China

bInstitute of Science and Technology, São Paulo State University (UNESP), Av. Três de Março 511, 18087-180, Sorocaba, SP, Brazil

*Correspondence: wenhao.su@cau.edu.cn

Table S1. Raw dataset of AgNPs’ physicochemical features and antimicrobial properties

| Number | Material |  |  |  |  |  | Bacteria |  |  | MIC | Link |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Synthesis | Size | Shape | SA/V | Sphericity | Zeta | Bacterium | Genus | Gram |  |  |
| 1 | Commercial | 16.00 | Irregular | 0.56 | 0.67 | NAN | Citrobacter amalonaticus UPMR bio1 | Other | - | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 2 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Pseudomonas sp UPMR 040 | Pseudomonas sp. | - | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 3 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Acinetobacter baumannii | Other | - | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 4 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Acinetobacter baumannii ATCC 19606 | Other | - | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 5 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Bacillus pumilus UMPR Skb2 | Bacillus sp. | + | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 6 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Bacillus cereus UPMR Skb7 | Bacillus sp. | + | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 7 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Acinetobacter baumannii multiresistant | Other | - | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 8 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Acinetobacter brisouii UPMR Skb1 | Other | - | 40.00 | https://doi.org/10.7717/peerj.6418 |
| 9 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Actinomyces odontolyticus | Other | + | 36.00 | https://doi.org/10.7717/peerj.6418 |
| 10 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Bacillus pumilus UPMR Sm1 | Bacillus sp. | + | 28.00 | https://doi.org/10.7717/peerj.6418 |
| 11 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Aggregatibacter actinomycetemcomitans ATCC 29523 | Other | - | 14.00 | https://doi.org/10.7717/peerj.6418 |
| 12 | Commercial | 16.00 | Spherical | 0.38 | 1.00 | NAN | Bacillus cereus UPMR1021 | Bacillus sp. | + | 12.00 | https://doi.org/10.7717/peerj.6418 |
| 13 | Green | 12.50 | Spherical | 0.48 | 1.00 | NAN | Aggregatibacter actinomycetemcomitans ATCC 29523 | Other | - | 15.62 | https://doi.org/10.1016/j.micpath.2018.01.033 |
| 14 | Green | 45.00 | Spherical | 0.13 | 1.00 | NAN | Klebsiella pneumoniae ATCC 100603 | Klebsiella sp. | - | 4.00 | https://doi.org/10.1007/s00449-013-1070-8 |
| 15 | Green | 45.00 | Spherical | 0.13 | 1.00 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 1.40 | https://doi.org/10.1007/s00449-013-1070-8 |
| 16 | Green | 45.00 | Spherical | 0.13 | 1.00 | NAN | Escherichia coli | Escherichia sp. | - | 2.00 | https://doi.org/10.1007/s00449-013-1070-8 |
| 17 | Green | 45.00 | Spherical | 0.13 | 1.00 | NAN | Aggregatibacter actinomycetemcomitans ATCC 29523 | Other | - | 2.00 | https://doi.org/10.1007/s00449-013-1070-8 |
| 18 | Green | 35.00 | Spherical | 0.17 | 1.00 | -26.30 | Escherichia coli | Escherichia sp. | - | 6.25 | https://doi.org/10.1080%2F20477724.2017.1390829 |
| 19 | Green | 35.00 | Spherical | 0.17 | 1.00 | -26.30 | Staphylococcus aureus | Staphylococcus sp. | + | 12.50 | https://doi.org/10.1080%2F20477724.2017.1390829 |
| 20 | Green | 35.00 | Spherical | 0.17 | 1.00 | -26.30 | Klebsiella pneumoniae | Klebsiella sp. | - | 3.12 | https://doi.org/10.1080%2F20477724.2017.1390829 |
| 21 | Green | 35.00 | Spherical | 0.17 | 1.00 | -26.30 | Pseudomonas aeruginosa | Pseudomonas sp. | - | 3.12 | https://doi.org/10.1080%2F20477724.2017.1390829 |
| 22 | Green | 35.50 | Spherical | 0.17 | 1.00 | NAN | Escherichia coli MTCC 9537 | Escherichia sp. | - | 14.00 | https://doi.org/10.1007/s40097-016-0197-y |
| 23 | Green | 35.50 | Spherical | 0.17 | 1.00 | NAN | Klebsiella pneumoniae MTCC 109 | Klebsiella sp. | - | 12.00 | https://doi.org/10.1007/s40097-016-0197-y |
| 24 | Green | 35.50 | Spherical | 0.17 | 1.00 | NAN | Staphylococcus aureus MTCC 96 | Staphylococcus sp. | + | 15.00 | https://doi.org/10.1007/s40097-016-0197-y |
| 25 | Green | 35.50 | Spherical | 0.17 | 1.00 | NAN | Pseudomonas aeruginosa MTCC 1688 | Pseudomonas sp. | - | 10.00 | https://doi.org/10.1007/s40097-016-0197-y |
| 26 | Green | 24.00 | Spherical | 0.25 | 1.00 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 9.38 | https://doi.org/10.1186/s12951-014-0040-x |
| 27 | Green | 16.00 | Triangular | 1.68 | 0.51 | NAN | Escherichia coli MC-2 | Escherichia sp. | - | 4.00 | https://doi.org/10.1016/j.arabjc.2015.08.008 |
| 28 | Green | 16.00 | Triangular | 1.68 | 0.51 | NAN | Staphylococcus aureus MMC-20 | Staphylococcus sp. | + | 8.00 | https://doi.org/10.1016/j.arabjc.2015.08.008 |
| 29 | Green | 17.20 | Spherical | 0.35 | 1.00 | -28.50 | Bacillus subtilis | Bacillus sp. | + | 0.13 | https://doi.org/10.1021/acsomega.2c01922 |
| 30 | Green | 17.20 | Spherical | 0.35 | 1.00 | -27.50 | Escherichia coli K12 | Escherichia sp. | - | 0.13 | https://doi.org/10.1021/acsomega.2c01922 |
| 31 | Green | 17.20 | Spherical | 0.35 | 1.00 | -26.50 | Escherichia coli DH5α | Escherichia sp. | - | 0.13 | https://doi.org/10.1021/acsomega.2c01922 |
| 32 | Green | 17.20 | Spherical | 0.35 | 1.00 | -25.50 | Enteropathogenic Escherichia coli EPEC | Escherichia sp. | - | 0.13 | https://doi.org/10.1021/acsomega.2c01922 |
| 33 | Green | 17.20 | Spherical | 0.35 | 1.00 | -24.50 | Aggregatibacter actinomycetemcomitans ATCC 33384 | Other | - | 0.13 | https://doi.org/10.1021/acsomega.2c01922 |
| 34 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | -22.80 | Escherichia coli MTCC 443 | Escherichia sp. | - | 20.00 | https://doi.org/10.1039/C3RA44507K |
| 35 | Chemical | 7.00 | Spherical | 0.86 | 1.00 | -27.30 | Escherichia coli MTCC 443 | Escherichia sp. | - | 20.00 | https://doi.org/10.1039/C3RA44507K |
| 36 | Chemical | 10.00 | Spherical | 0.60 | 1.00 | -30.20 | Escherichia coli MTCC 443 | Escherichia sp. | - | 30.00 | https://doi.org/10.1039/C3RA44507K |
| 37 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | -34.00 | Escherichia coli MTCC 443 | Escherichia sp. | - | 30.00 | https://doi.org/10.1039/C3RA44507K |
| 38 | Chemical | 20.00 | Spherical | 0.30 | 1.00 | -35.10 | Escherichia coli MTCC 443 | Escherichia sp. | - | 40.00 | https://doi.org/10.1039/C3RA44507K |
| 39 | Chemical | 30.00 | Spherical | 0.20 | 1.00 | -33.70 | Escherichia coli MTCC 443 | Escherichia sp. | - | 50.00 | https://doi.org/10.1039/C3RA44507K |
| 40 | Chemical | 50.00 | Spherical | 0.12 | 1.00 | -41.80 | Escherichia coli MTCC 443 | Escherichia sp. | - | 80.00 | https://doi.org/10.1039/C3RA44507K |
| 41 | Chemical | 63.00 | Spherical | 0.10 | 1.00 | -48.50 | Escherichia coli MTCC 443 | Escherichia sp. | - | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 42 | Chemical | 85.00 | Spherical | 0.07 | 1.00 | -52.40 | Escherichia coli MTCC 443 | Escherichia sp. | - | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 43 | Chemical | 100.00 | Spherical | 0.06 | 1.00 | -53.10 | Escherichia coli MTCC 443 | Escherichia sp. | - | 110.00 | https://doi.org/10.1039/C3RA44507K |
| 44 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | -22.80 | Escherichia coli MTCC 739 | Escherichia sp. | - | 60.00 | https://doi.org/10.1039/C3RA44507K |
| 45 | Chemical | 7.00 | Spherical | 0.86 | 1.00 | -27.30 | Escherichia coli MTCC 739 | Escherichia sp. | - | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 46 | Chemical | 10.00 | Spherical | 0.60 | 1.00 | -30.20 | Escherichia coli MTCC 739 | Escherichia sp. | - | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 47 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | -34.00 | Escherichia coli MTCC 739 | Escherichia sp. | - | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 48 | Chemical | 20.00 | Spherical | 0.30 | 1.00 | -35.10 | Escherichia coli MTCC 739 | Escherichia sp. | - | 100.00 | https://doi.org/10.1039/C3RA44507K |
| 49 | Chemical | 30.00 | Spherical | 0.20 | 1.00 | -33.70 | Escherichia coli MTCC 739 | Escherichia sp. | - | 100.00 | https://doi.org/10.1039/C3RA44507K |
| 50 | Chemical | 50.00 | Spherical | 0.12 | 1.00 | -41.80 | Escherichia coli MTCC 739 | Escherichia sp. | - | 120.00 | https://doi.org/10.1039/C3RA44507K |
| 51 | Chemical | 63.00 | Spherical | 0.10 | 1.00 | -48.50 | Escherichia coli MTCC 739 | Escherichia sp. | - | 140.00 | https://doi.org/10.1039/C3RA44507K |
| 52 | Chemical | 85.00 | Spherical | 0.07 | 1.00 | -52.40 | Escherichia coli MTCC 739 | Escherichia sp. | - | 160.00 | https://doi.org/10.1039/C3RA44507K |
| 53 | Chemical | 100.00 | Spherical | 0.06 | 1.00 | -53.10 | Escherichia coli MTCC 739 | Escherichia sp. | - | 160.00 | https://doi.org/10.1039/C3RA44507K |
| 54 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | -22.80 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 30.00 | https://doi.org/10.1039/C3RA44507K |
| 55 | Chemical | 7.00 | Spherical | 0.86 | 1.00 | -27.30 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 40.00 | https://doi.org/10.1039/C3RA44507K |
| 56 | Chemical | 10.00 | Spherical | 0.60 | 1.00 | -30.20 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 40.00 | https://doi.org/10.1039/C3RA44507K |
| 57 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | -34.00 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 50.00 | https://doi.org/10.1039/C3RA44507K |
| 58 | Chemical | 20.00 | Spherical | 0.30 | 1.00 | -35.10 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 50.00 | https://doi.org/10.1039/C3RA44507K |
| 59 | Chemical | 30.00 | Spherical | 0.20 | 1.00 | -33.70 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 60.00 | https://doi.org/10.1039/C3RA44507K |
| 60 | Chemical | 50.00 | Spherical | 0.12 | 1.00 | -41.80 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 80.00 | https://doi.org/10.1039/C3RA44507K |
| 61 | Chemical | 63.00 | Spherical | 0.10 | 1.00 | -48.50 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 62 | Chemical | 85.00 | Spherical | 0.07 | 1.00 | -52.40 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 110.00 | https://doi.org/10.1039/C3RA44507K |
| 63 | Chemical | 100.00 | Spherical | 0.06 | 1.00 | -53.10 | Bacillus subtilis MTCC 441 | Bacillus sp. | + | 120.00 | https://doi.org/10.1039/C3RA44507K |
| 64 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | -22.80 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 70.00 | https://doi.org/10.1039/C3RA44507K |
| 65 | Chemical | 7.00 | Spherical | 0.86 | 1.00 | -27.30 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 70.00 | https://doi.org/10.1039/C3RA44507K |
| 66 | Chemical | 10.00 | Spherical | 0.60 | 1.00 | -30.20 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 80.00 | https://doi.org/10.1039/C3RA44507K |
| 67 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | -34.00 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 100.00 | https://doi.org/10.1039/C3RA44507K |
| 68 | Chemical | 20.00 | Spherical | 0.30 | 1.00 | -35.10 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 90.00 | https://doi.org/10.1039/C3RA44507K |
| 69 | Chemical | 30.00 | Spherical | 0.20 | 1.00 | -33.70 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 100.00 | https://doi.org/10.1039/C3RA44507K |
| 70 | Chemical | 50.00 | Spherical | 0.12 | 1.00 | -41.80 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 130.00 | https://doi.org/10.1039/C3RA44507K |
| 71 | Chemical | 63.00 | Spherical | 0.10 | 1.00 | -48.50 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 160.00 | https://doi.org/10.1039/C3RA44507K |
| 72 | Chemical | 85.00 | Spherical | 0.07 | 1.00 | -52.40 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 180.00 | https://doi.org/10.1039/C3RA44507K |
| 73 | Chemical | 100.00 | Spherical | 0.06 | 1.00 | -53.10 | Staphylococcus aureus NCIM 5021 | Staphylococcus sp. | + | 200.00 | https://doi.org/10.1039/C3RA44507K |
| 74 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | NAN | Bacteroides fragilis ATCC 25285 | Other | - | 25.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 75 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | NAN | Bacteroides uniformis | Other | - | 25.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 76 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | NAN | Streptococcus sanguis ATCC 10556 | Streptococcus sp. | + | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 77 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | NAN | Streptococcus mutans ATCC 35668 | Streptococcus sp. | + | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 78 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | NAN | Streptococcus mitis ATCC 15914 | Streptococcus sp. | + | 25.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 79 | Chemical | 5.00 | Spherical | 1.20 | 1.00 | NAN | Escherichia coli CCTCC AB 90054 | Escherichia sp. | - | 6.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 80 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | NAN | Bacteroides ureolyticus | Other | - | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 81 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | NAN | Bifidobacterium breve ATCC 15700 | Other | + | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 82 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | NAN | Streptococcus sanguis ATCC 10556 | Streptococcus sp. | + | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 83 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | NAN | Streptococcus mutans ATCC 35668 | Streptococcus sp. | + | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 84 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | NAN | Streptococcus mitis ATCC 15914 | Streptococcus sp. | + | 50.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 85 | Chemical | 15.00 | Spherical | 0.40 | 1.00 | NAN | Escherichia coli CCTCC AB 90054 | Escherichia sp. | - | 12.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 86 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Burkholderia sp UPMR 9 | Other | - | 200.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 87 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Chromobacterium violaceum UPMR Skb10 | Other | - | 100.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 88 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Streptococcus sanguis ATCC 10556 | Streptococcus sp. | + | 100.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 89 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Streptococcus mutans ATCC 35668 | Streptococcus sp. | + | 200.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 90 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Streptococcus mitis ATCC 15914 | Streptococcus sp. | + | 100.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 91 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Escherichia coli CCTCC AB 90054 | Escherichia sp. | - | 100.00 | https://doi.org/10.1007/s10856-013-4894-5 |
| 92 | Chemical | 55.00 | Spherical | 0.11 | 1.00 | NAN | Citrobacter | Other | - | 4.88 | https://doi.org/10.1155/2016/7135852 |
| 93 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Citrobacter agriculturist UPMR bio2 | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16011 |
| 94 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Enterobacter aerogenes | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16012 |
| 95 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Enterobacter sp UPMR rubber | Other | - | 40.00 | https://doi.org/10.7150/iJMS.16013 |
| 96 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Finegoldia magna | Other | + | 20.00 | https://doi.org/10.7150/iJMS.16014 |
| 97 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Fusobacterium necrophorum | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16015 |
| 98 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Fusobacterium nucleatum ATCC 25586 | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16016 |
| 99 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Fusobacterium nucleatum ATCC 25586 | Other | - | 10.00 | https://doi.org/10.7150/iJMS.16017 |
| 100 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Fusobacterium nucleatum ATCC 25586 | Other | - | 20.00 | https://doi.org/10.7150/iJMS.16018 |
| 101 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Fusobacterium nucleatum ATCC 25586 | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16019 |
| 102 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Listeria monocytogenes ATCC 7644 | Other | + | 5.00 | https://doi.org/10.7150/iJMS.16020 |
| 103 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Paenibacillus sp UPMR 1004 | Other | + | 100.00 | https://doi.org/10.7150/iJMS.16021 |
| 104 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Parabacteroides distasonis | Other | - | 100.00 | https://doi.org/10.7150/iJMS.16022 |
| 105 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Peptococcus levii ATCC 29147 | Other | - | 40.00 | https://doi.org/10.7150/iJMS.16023 |
| 106 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Peptostreptococcus anaerobius ATCC 25286 | Other | + | 5.00 | https://doi.org/10.7150/iJMS.16024 |
| 107 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Peptostreptococcus asaccharolytica | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16025 |
| 108 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Peptostreptococcus buccalis | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16026 |
| 109 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Peptostreptococcus micra | Other | + | 5.00 | https://doi.org/10.7150/iJMS.16027 |
| 110 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Porphyromonas gingivalis | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16028 |
| 111 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Prevotella intermedia | Other | - | 5.00 | https://doi.org/10.7150/iJMS.16029 |
| 112 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Prevotella loescheii ATCC 15930 | Other | - | 10.00 | https://doi.org/10.7150/iJMS.16030 |
| 113 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Staphylococcus aureus ATCC 25923 | Staphylococcus sp. | + | 2.50 | https://doi.org/10.7150/iJMS.16031 |
| 114 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Staphylococcus aureus ATCC 6538 | Staphylococcus sp. | + | 2.50 | https://doi.org/10.7150/iJMS.16032 |
| 115 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Staphylococcus aureus ATCC 6538/P | Staphylococcus sp. | + | 10.00 | https://doi.org/10.7150/iJMS.16033 |
| 116 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Staphylococcus epidermidis ATCC 14990 | Staphylococcus sp. | + | 0.31 | https://doi.org/10.7150/iJMS.16034 |
| 117 | Commercial | 11.20 | Spherical | 0.54 | 1.00 | -33.90 | Streptococcus mutans ATCC 29175 | Streptococcus sp. | + | 10.00 | https://doi.org/10.7150/iJMS.16035 |
| 118 | Green | 12.50 | Spherical | 0.48 | 1.00 | NAN | Propionibacterium acnes | Other | + | 7.81 | https://doi.org/10.1016/j.jphotobiol.2018.02.005 |
| 119 | Green | 12.50 | Spherical | 0.48 | 1.00 | -15.70 | Escherichia coli ATCC 8739 | Escherichia sp. | - | 64.00 | https://doi.org/10.1007/s11274-017-2406-3 |
| 120 | Green | 12.50 | Spherical | 0.48 | 1.00 | -15.70 | Klebsiella pneumoniae ATCC 700603 | Klebsiella sp. | - | 256.00 | https://doi.org/10.1007/s11274-017-2406-3 |
| 121 | Green | 12.50 | Spherical | 0.48 | 1.00 | -15.70 | Pseudomonas aeruginosa ATCC 10145 | Pseudomonas sp. | - | 16.00 | https://doi.org/10.1007/s11274-017-2406-3 |
| 122 | Green | 12.50 | Spherical | 0.48 | 1.00 | -15.70 | Staphylococcus aureus ATCC 6538 | Staphylococcus sp. | + | 256.00 | https://doi.org/10.1007/s11274-017-2406-3 |
| 123 | Green | 12.50 | Spherical | 0.48 | 1.00 | -15.70 | Bacillus subtilis PCM 2021 | Bacillus sp. | + | 64.00 | https://doi.org/10.1007/s11274-017-2406-3 |
| 124 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Escherichia coli ATCC8739 | Escherichia sp. | - | 6.25 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 125 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Propionibacterium granulosum | Other | + | 6.25 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 126 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Klebsiella pneumoniae ATCC700603 | Klebsiella sp. | - | 6.25 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 127 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Bacillus subtilis PCM2021 | Bacillus sp. | + | 6.25 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 128 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Staphylococcus aureus ATCC6338 | Staphylococcus sp. | + | 6.25 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 129 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Pseudomonas aeruginosa ATCC10145 | Pseudomonas sp. | - | 25.00 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 130 | Green | 23.00 | Spherical | 0.26 | 1.00 | 0.00 | Proteus mirabilis | Other | - | 50.00 | https://doi.org/10.1016/j.jmii.2016.03.002 |
| 131 | Green | 14.00 | Spherical | 0.43 | 1.00 | -16.60 | Escherichia coli ATCC8739 | Escherichia sp. | - | 70.00 | https://doi.org/10.1049/iet-nbt.2016.0112 |
| 132 | Green | 14.00 | Spherical | 0.43 | 1.00 | -16.60 | Staphylococcus aureus ATCC6338 | Staphylococcus sp. | + | 40.00 | https://doi.org/10.1049/iet-nbt.2016.0112 |
| 133 | Green | 14.00 | Spherical | 0.43 | 1.00 | -16.60 | Bacillus subtilis PCM2021 | Bacillus sp. | + | 40.00 | https://doi.org/10.1049/iet-nbt.2016.0112 |
| 134 | Green | 12.70 | Spherical | 0.47 | 1.00 | -24.10 | Staphylococcus aureus ATCC6338 | Staphylococcus sp. | + | 70.00 | https://doi.org/10.1002/jobm.201500516 |
| 135 | Green | 12.70 | Spherical | 0.47 | 1.00 | -24.10 | Bacillus subtilis PCM2021 | Bacillus sp. | + | 90.00 | https://doi.org/10.1002/jobm.201500516 |
| 136 | Green | 12.70 | Spherical | 0.47 | 1.00 | -24.10 | Klebsiella pneumoniae ATCC700603 | Klebsiella sp. | - | 90.00 | https://doi.org/10.1002/jobm.201500516 |
| 137 | Green | 12.70 | Spherical | 0.47 | 1.00 | -24.10 | Escherichia coli ATCC8739 | Escherichia sp. | - | 90.00 | https://doi.org/10.1002/jobm.201500516 |
| 138 | Green | 12.70 | Spherical | 0.47 | 1.00 | -24.10 | Pseudomonas aeruginosa ATCC10145 | Pseudomonas sp. | - | 90.00 | https://doi.org/10.1002/jobm.201500516 |
| 139 | Green | 15.90 | Spherical | 0.38 | 1.00 | -16.60 | Staphylococcus aureus ATCC6338 | Staphylococcus sp. | + | 90.00 | https://doi.org/10.1002/jobm.201500516 |
| 140 | Green | 15.90 | Spherical | 0.38 | 1.00 | -16.60 | Bacillus subtilis PCM2021 | Bacillus sp. | + | 50.00 | https://doi.org/10.1002/jobm.201500516 |
| 141 | Green | 15.90 | Spherical | 0.38 | 1.00 | -16.60 | Klebsiella pneumoniae ATCC700603 | Klebsiella sp. | - | 60.00 | https://doi.org/10.1002/jobm.201500516 |
| 142 | Green | 15.90 | Spherical | 0.38 | 1.00 | -16.60 | Escherichia coli ATCC8739 | Escherichia sp. | - | 40.00 | https://doi.org/10.1002/jobm.201500516 |
| 143 | Green | 15.90 | Spherical | 0.38 | 1.00 | -16.60 | Pseudomonas aeruginosa ATCC10145 | Pseudomonas sp. | - | 40.00 | https://doi.org/10.1002/jobm.201500516 |
| 144 | Chemical | 12.50 | Spherical | 0.48 | 1.00 | NAN | Pseudomonas aeruginosa resistant | Pseudomonas sp. | - | 2.60 | https://doi.org/10.2147/IJN.S191340 |
| 145 | Chemical | 12.50 | Spherical | 0.48 | 1.00 | NAN | Pseudomonas aeruginosa multidrug-resistant | Pseudomonas sp. | - | 2.29 | https://doi.org/10.2147/IJN.S191340 |
| 146 | Green | 11.00 | Spherical | 0.55 | 1.00 | NAN | Pseudomonas aeruginosa MDR12 | Pseudomonas sp. | - | 1.00 | https://doi.org/10.3390/ijms18030569 |
| 147 | Green | 11.00 | Spherical | 0.55 | 1.00 | NAN | Staphylococcus aureus MDR13 | Staphylococcus sp. | + | 2.00 | https://doi.org/10.3390/ijms18030569 |
| 148 | Commercial | 35.00 | Spherical | 0.17 | 1.00 | -18.00 | Escherichia coli DH5α | Escherichia sp. | - | 10.00 | https://doi.org/10.1371/journal.pone.0224904 |
| 149 | Commercial | 35.00 | Spherical | 0.17 | 1.00 | -18.00 | Proteus mirabilis ATCC 25933 | Other | - | 10.00 | https://doi.org/10.1371/journal.pone.0224904 |
| 150 | Commercial | 35.00 | Spherical | 0.17 | 1.00 | -18.00 | Staphylococcus aureus | Staphylococcus sp. | + | 12.00 | https://doi.org/10.1371/journal.pone.0224904 |
| 151 | Commercial | 35.00 | Spherical | 0.17 | 1.00 | -18.00 | Bacillus subtilis | Bacillus sp. | + | 11.00 | https://doi.org/10.1371/journal.pone.0224904 |
| 152 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Staphylococcus aureus ATCC 25923 | Staphylococcus sp. | + | 10.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 153 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Methicillin-resistant Staphylococcus aureus ATCC 4330 | MRSA | + | 10.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 154 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Streptococcus mutans ATCC 25175 | Streptococcus sp. | + | 5.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 155 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Streptococcus oralis ATCC 35037 | Streptococcus sp. | + | 5.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 156 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Streptococcus gordonii ATCC 49818 | Streptococcus sp. | + | 10.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 157 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Enterococcus faecalis 700802 | Other | + | 10.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 158 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Escherichia coli ATCC 25922 | Escherichia sp. | - | 5.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 159 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Proteus vulgaris | Other | - | 2.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 160 | Green | 26.00 | Spherical | 0.23 | 1.00 | -8.90 | Pseudomonas aeruginosa ATCC 27853 | Pseudomonas sp. | - | 2.00 | https://doi.org/10.3389/fmicb.2020.01074 |
| 161 | Commercial | 36.00 | Irregular | 0.25 | 0.67 | NAN | Escherichia coli ATCC 25922 | Escherichia sp. | - | 310.00 | https://doi.org/10.1590/S1678-9946201860018 |
| 162 | Chemical | 19.00 | Cubic | 0.32 | 0.81 | -31.50 | Escherichia coli ATCC 35218 | Escherichia sp. | - | 400.00 | https://doi.org/10.1038/s41598-020-68290-x |
| 163 | Chemical | 19.00 | Cubic | 0.32 | 0.81 | -31.50 | Klebsiella pneumoniae ATCC 700603 | Klebsiella sp. | - | 300.00 | https://doi.org/10.1038/s41598-020-68290-x |
| 164 | Chemical | 19.00 | Cubic | 0.32 | 0.81 | -31.50 | Methicillin-resistant Staphylococcus aureus ATCC 25923 | MRSA | + | 300.00 | https://doi.org/10.1038/s41598-020-68290-x |
| 165 | Green | 6.00 | Spherical | 1.00 | 1.00 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 0.59 | https://doi.org/10.1186/1556-276X-9-373 |
| 166 | Green | 6.00 | Spherical | 1.00 | 1.00 | NAN | Proteus vulgaris | Other | - | 0.60 | https://doi.org/10.1186/1556-276X-9-373 |
| 167 | Green | 6.00 | Spherical | 1.00 | 1.00 | NAN | Staphylococcus aureus | Staphylococcus sp. | + | 0.75 | https://doi.org/10.1186/1556-276X-9-373 |
| 168 | Green | 6.00 | Spherical | 1.00 | 1.00 | NAN | Streptococcus pneumoniae | Streptococcus sp. | + | 0.76 | https://doi.org/10.1186/1556-276X-9-373 |
| 169 | Green | 40.00 | Spherical | 0.15 | 1.00 | NAN | Bacillus sp | Bacillus sp. | + | 30.00 | https://doi.org/10.1016/j.bcab.2019.101037 |
| 170 | Green | 40.00 | Spherical | 0.15 | 1.00 | NAN | Staphylococcus aureus | Staphylococcus sp. | + | 30.00 | https://doi.org/10.1016/j.bcab.2019.101037 |
| 171 | Green | 40.00 | Spherical | 0.15 | 1.00 | NAN | Escherichia coli | Escherichia sp. | - | 40.00 | https://doi.org/10.1016/j.bcab.2019.101037 |
| 172 | Green | 40.00 | Spherical | 0.15 | 1.00 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 40.00 | https://doi.org/10.1016/j.bcab.2019.101037 |
| 173 | Green | 40.00 | Spherical | 0.15 | 1.00 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 40.00 | https://doi.org/10.1016/j.bcab.2019.101037 |
| 174 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Pseudomonas aeruginosa ATCC 9027 | Pseudomonas sp. | - | 6.25 | https://doi.org/10.1021/mp900056g |
| 175 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Proteus vulgaris | Other | - | 6.25 | https://doi.org/10.1021/mp900056g |
| 176 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Proteus vulgaris NCIB 4157 | Other | - | 6.25 | https://doi.org/10.1021/mp900056g |
| 177 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Klebsiella aerogenes ATCC 1950 | Klebsiella sp. | - | 6.25 | https://doi.org/10.1021/mp900056g |
| 178 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Ralstonia solanacearum | Other | - | 6.25 | https://doi.org/10.1021/mp900056g |
| 179 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Bacillus subtilis ATCC 6633 | Bacillus sp. | + | 6.25 | https://doi.org/10.1021/mp900056g |
| 180 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Staphylococcus aureus ATCC 6538 | Staphylococcus sp. | + | 12.50 | https://doi.org/10.1021/mp900056g |
| 181 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Staphylococcus epidermidis ATCC 12228 | Staphylococcus sp. | + | 6.25 | https://doi.org/10.1021/mp900056g |
| 182 | Biological | 13.50 | Spherical | 0.44 | 1.00 | NAN | Escherichia coli ATCC 117 | Escherichia sp. | - | 6.25 | https://doi.org/10.1021/mp900056g |
| 183 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Enterococcus faecalis CCM 4224 | Other | + | 6.75 | https://doi.org/10.1021/jp711616v |
| 184 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Staphylococcus aureus CCM 3953 | Staphylococcus sp. | + | 3.38 | https://doi.org/10.1021/jp711616v |
| 185 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Escherichia coli CCM 3954 | Escherichia sp. | - | 1.69 | https://doi.org/10.1021/jp711616v |
| 186 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Pseudomonas aeruginosa CCM 3955 | Pseudomonas sp. | - | 3.38 | https://doi.org/10.1021/jp711616v |
| 187 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Staphylococcus epidermidis | Staphylococcus sp. | + | 1.69 | https://doi.org/10.1021/jp711616v |
| 188 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Methicillin-resistant Staphylococcus epidermidis | MRSA | + | 1.69 | https://doi.org/10.1021/jp711616v |
| 189 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Methicillin-resistant Staphylococcus aureus | MRSA | + | 3.38 | https://doi.org/10.1021/jp711616v |
| 190 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Ralstonia solanacearum NAIMCC-B-01626 | Other | - | 6.75 | https://doi.org/10.1021/jp711616v |
| 191 | Chemical | 26.00 | Spherical | 0.23 | 1.00 | -25.00 | Klebsiella pneumoniae ESBL | Klebsiella sp. | - | 6.75 | https://doi.org/10.1021/jp711616v |
| 192 | Chemical | 8.45 | Spherical | 0.71 | 1.00 | NAN | Staphylococcus aureus | Staphylococcus sp. | + | 398.00 | https://doi.org/10.1002/jbm.a.35005 |
| 193 | Chemical | 8.45 | Spherical | 0.71 | 1.00 | NAN | Bacillus megaterium | Bacillus sp. | + | 199.00 | https://doi.org/10.1002/jbm.a.35005 |
| 194 | Chemical | 8.45 | Spherical | 0.71 | 1.00 | NAN | Salmonella abony NCTC 6017 | Other | - | 199.00 | https://doi.org/10.1002/jbm.a.35005 |
| 195 | Chemical | 8.45 | Spherical | 0.71 | 1.00 | NAN | Salmonella enterica serovar Typhimurium | Other | - | 199.00 | https://doi.org/10.1002/jbm.a.35005 |
| 196 | Chemical | 8.07 | Spherical | 0.74 | 1.00 | NAN | Staphylococcus aureus | Staphylococcus sp. | + | 150.00 | https://doi.org/10.1002/jbm.a.35005 |
| 197 | Chemical | 8.07 | Spherical | 0.74 | 1.00 | NAN | Bacillus megaterium | Bacillus sp. | + | 75.00 | https://doi.org/10.1002/jbm.a.35005 |
| 198 | Chemical | 8.07 | Spherical | 0.74 | 1.00 | NAN | Salmonella enterica serovar Typhimurium ATCC SC14028 | Other | - | 100.00 | https://doi.org/10.1002/jbm.a.35005 |
| 199 | Chemical | 8.07 | Spherical | 0.74 | 1.00 | NAN | Salmonella infantis | Other | - | 100.00 | https://doi.org/10.1002/jbm.a.35005 |
| 200 | Green | 90.00 | Spherical | 0.07 | 1.00 | -25.30 | Staphylococcus aureus | Staphylococcus sp. | + | 65.00 | https://doi.org/10.1080/21691401.2022.2149543 |
| 201 | Green | 90.00 | Spherical | 0.07 | 1.00 | -24.30 | Escherichia coli | Escherichia sp. | - | 70.00 | https://doi.org/10.1080/21691401.2022.2149543 |
| 202 | Green | 90.00 | Spherical | 0.07 | 1.00 | -23.30 | Pseudomonas aeruginosa | Pseudomonas sp. | - | 75.00 | https://doi.org/10.1080/21691401.2022.2149543 |
| 203 | Green | 90.00 | Spherical | 0.07 | 1.00 | -22.30 | Klebsiella pneumoniae | Klebsiella sp. | - | 60.00 | https://doi.org/10.1080/21691401.2022.2149543 |
| 204 | Green | 20.34 | Spherical | 0.29 | 1.00 | NAN | Staphylococcus aureus ATCC 25923 | Staphylococcus sp. | + | 128.00 | https://doi.org/10.1016/j.heliyon.2020.e03624 |
| 205 | Green | 20.34 | Spherical | 0.29 | 1.00 | NAN | Salmonella typhi | Other | - | 64.00 | https://doi.org/10.1016/j.heliyon.2020.e03624 |
| 206 | Green | 20.34 | Spherical | 0.29 | 1.00 | NAN | Escherichia coli ATCC 25922 | Escherichia sp. | - | 16.00 | https://doi.org/10.1016/j.heliyon.2020.e03624 |
| 207 | Green | 20.34 | Spherical | 0.29 | 1.00 | NAN | Pseudomonas aeruginosa ATCC 27853 | Pseudomonas sp. | - | 32.00 | https://doi.org/10.1016/j.heliyon.2020.e03624 |
| 208 | Green | 4.50 | Spherical | 1.33 | 1.00 | -32.70 | Staphylococcus aureus 25923 | Staphylococcus sp. | + | 10.00 | https://doi.org/10.1016/j.arabjc.2014.10.036 |
| 209 | Green | 4.50 | Spherical | 1.33 | 1.00 | -32.70 | Pseudomonas aeruginosa 27853 | Pseudomonas sp. | - | 5.00 | https://doi.org/10.1016/j.arabjc.2014.10.036 |
| 210 | Green | 4.50 | Spherical | 1.33 | 1.00 | -32.70 | Escherichia coli 25922 | Escherichia sp. | - | 2.00 | https://doi.org/10.1016/j.arabjc.2014.10.036 |
| 211 | Green | 4.50 | Spherical | 1.33 | 1.00 | -32.70 | Escherichia coli 35218 | Escherichia sp. | - | 2.00 | https://doi.org/10.1016/j.arabjc.2014.10.036 |
| 212 | Green | 37.50 | Spherical | 0.16 | 1.00 | -34.00 | Escherichia coli | Escherichia sp. | - | 50.00 | https://doi.org/10.3390/molecules26195762 |
| 213 | Green | 37.50 | Spherical | 0.16 | 1.00 | -34.00 | Pseudomonas aeruginosa | Pseudomonas sp. | - | 50.00 | https://doi.org/10.3390/molecules26195762 |
| 214 | Green | 37.50 | Spherical | 0.16 | 1.00 | -34.00 | Salmonella typhi | Other | - | 75.00 | https://doi.org/10.3390/molecules26195762 |
| 215 | Green | 37.50 | Spherical | 0.16 | 1.00 | -34.00 | Bacillus subtilis | Bacillus sp. | + | 100.00 | https://doi.org/10.3390/molecules26195762 |
| 216 | Green | 37.50 | Spherical | 0.16 | 1.00 | -34.00 | Staphylococcus aureus | Staphylococcus sp. | + | 125.00 | https://doi.org/10.3390/molecules26195762 |
| 217 | Physical | 3.10 | Spherical | 1.94 | 1.00 | NAN | Pseudomonas aeruginosa 620 | Pseudomonas sp. | - | 27.00 | https://doi.org/10.1371/journal.pone.0131178 |
| 218 | Physical | 3.10 | Spherical | 1.94 | 1.00 | NAN | Escherichia coli 157 | Escherichia sp. | - | 36.00 | https://doi.org/10.1371/journal.pone.0131178 |
| 219 | Physical | 3.10 | Spherical | 1.94 | 1.00 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 27.00 | https://doi.org/10.1371/journal.pone.0131178 |
| 220 | Physical | 3.10 | Spherical | 1.94 | 1.00 | NAN | Methicillin-resistant Staphylococcus epidermidis | MRSA | + | 30.00 | https://doi.org/10.1371/journal.pone.0131178 |
| 221 | Green | 29.00 | Spherical | 0.21 | 1.00 | NAN | Salmonella typhimurium | Other | - | 200.00 | https://doi.org/10.1007/s12088-019-00801-5 |
| 222 | Chemical | 36.16 | Spherical | 0.17 | 1.00 | 0.00 | Escherichia coli O157:H7 | Escherichia sp. | - | 0.25 | https://doi.org/10.2147/IJN.S57156 |
| 223 | Chemical | 113.37 | Spherical | 0.05 | 1.00 | 0.00 | Escherichia coli O157:H7 | Escherichia sp. | - | 10.00 | https://doi.org/10.2147/IJN.S57157 |
| 224 | Chemical | 78.50 | Spherical | 0.08 | 1.00 | 0.00 | Escherichia coli O157:H7 | Escherichia sp. | - | 10.00 | https://doi.org/10.2147/IJN.S57158 |
| 225 | Chemical | 36.16 | Spherical | 0.17 | 1.00 | 0.00 | Methicillin-resistant Staphylococcus aureus | MRSA | + | 0.25 | https://doi.org/10.2147/IJN.S57159 |
| 226 | Chemical | 113.37 | Spherical | 0.05 | 1.00 | 0.00 | Methicillin-resistant Staphylococcus aureus | MRSA | + | 0.50 | https://doi.org/10.2147/IJN.S57160 |
| 227 | Chemical | 78.50 | Spherical | 0.08 | 1.00 | 0.00 | Methicillin-resistant Staphylococcus aureus | MRSA | + | 0.25 | https://doi.org/10.2147/IJN.S57161 |
| 228 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Staphylococcus aureus CCM 3953 | Staphylococcus sp. | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 229 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Escherichia coli CCM 3954 | Escherichia sp. | - | 27.00 | https://doi.org/10.1021/jp063826h |
| 230 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Pseudomonas aeruginosa CCM 3955 | Pseudomonas sp. | - | 27.00 | https://doi.org/10.1021/jp063826h |
| 231 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 13.50 | https://doi.org/10.1021/jp063826h |
| 232 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Staphylococcus epidermidis | Staphylococcus sp. | + | 13.50 | https://doi.org/10.1021/jp063826h |
| 233 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Methicillin-resistant Staphylococcus epidermidis | MRSA | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 234 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 27.00 | https://doi.org/10.1021/jp063826h |
| 235 | Chemical | 44.00 | Cubic | 0.14 | 0.81 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 27.00 | https://doi.org/10.1021/jp063826h |
| 236 | Chemical | 50.00 | Cubic | 0.12 | 0.81 | NAN | Staphylococcus aureus CCM 3953 | Staphylococcus sp. | + | 54.00 | https://doi.org/10.1021/jp063826h |
| 237 | Chemical | 50.00 | Cubic | 0.12 | 0.81 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 27.00 | https://doi.org/10.1021/jp063826h |
| 238 | Chemical | 50.00 | Cubic | 0.12 | 0.81 | NAN | Staphylococcus epidermidis | Staphylococcus sp. | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 239 | Chemical | 50.00 | Cubic | 0.12 | 0.81 | NAN | Methicillin-resistant Staphylococcus epidermidis | MRSA | + | 54.00 | https://doi.org/10.1021/jp063826h |
| 240 | Chemical | 50.00 | Cubic | 0.12 | 0.81 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 54.00 | https://doi.org/10.1021/jp063826h |
| 241 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Enterococcus faecalis CCM 4224 | Other | + | 13.50 | https://doi.org/10.1021/jp063826h |
| 242 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Staphylococcus aureus CCM 3953 | Staphylococcus sp. | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 243 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Escherichia coli CCM 3954 | Escherichia sp. | - | 3.38 | https://doi.org/10.1021/jp063826h |
| 244 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Pseudomonas aeruginosa CCM 3955 | Pseudomonas sp. | - | 6.75 | https://doi.org/10.1021/jp063826h |
| 245 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 3.38 | https://doi.org/10.1021/jp063826h |
| 246 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Staphylococcus epidermidis | Staphylococcus sp. | + | 1.69 | https://doi.org/10.1021/jp063826h |
| 247 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Methicillin-resistant Staphylococcus epidermidis | MRSA | + | 1.69 | https://doi.org/10.1021/jp063826h |
| 248 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 249 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Enterococcus faecium | Other | + | 13.50 | https://doi.org/10.1021/jp063826h |
| 250 | Chemical | 25.00 | Cubic | 0.24 | 0.81 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 6.75 | https://doi.org/10.1021/jp063826h |
| 251 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Enterococcus faecalis CCM 4224 | Other | + | 54.00 | https://doi.org/10.1021/jp063826h |
| 252 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Staphylococcus aureus CCM 3953 | Staphylococcus sp. | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 253 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Escherichia coli CCM 3954 | Escherichia sp. | - | 27.00 | https://doi.org/10.1021/jp063826h |
| 254 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Pseudomonas aeruginosa CCM 3955 | Pseudomonas sp. | - | 13.50 | https://doi.org/10.1021/jp063826h |
| 255 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 13.50 | https://doi.org/10.1021/jp063826h |
| 256 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Staphylococcus epidermidis | Staphylococcus sp. | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 257 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Methicillin-resistant Staphylococcus epidermidis | MRSA | + | 6.75 | https://doi.org/10.1021/jp063826h |
| 258 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 27.00 | https://doi.org/10.1021/jp063826h |
| 259 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Enterococcus faecium | Other | + | 54.00 | https://doi.org/10.1021/jp063826h |
| 260 | Chemical | 35.00 | Cubic | 0.17 | 0.81 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 54.00 | https://doi.org/10.1021/jp063826h |
| 261 | Physical | 2.20 | Spherical | 2.73 | 1.00 | -33.00 | Escherichia coli XL1Blue | Escherichia sp. | - | 8.40 | https://doi.org/10.3762/bjnano.7.40 |
| 262 | Physical | 2.20 | Spherical | 2.73 | 1.00 | -33.00 | Bacillus subtilis 168 | Bacillus sp. | + | 1.70 | https://doi.org/10.3762/bjnano.7.40 |
| 263 | Physical | 2.20 | Spherical | 2.73 | 1.00 | -50.00 | Escherichia coli XL1Blue | Escherichia sp. | - | 9.20 | https://doi.org/10.3762/bjnano.7.40 |
| 264 | Physical | 2.20 | Spherical | 2.73 | 1.00 | -50.00 | Bacillus subtilis 168 | Bacillus sp. | + | 9.20 | https://doi.org/10.3762/bjnano.7.40 |
| 265 | Physical | 3.30 | Spherical | 1.82 | 1.00 | -55.00 | Escherichia coli XL1Blue | Escherichia sp. | - | 9.20 | https://doi.org/10.3762/bjnano.7.40 |
| 266 | Physical | 3.30 | Spherical | 1.82 | 1.00 | -55.00 | Bacillus subtilis 168 | Bacillus sp. | + | 1.00 | https://doi.org/10.3762/bjnano.7.40 |
| 267 | Physical | 6.10 | Spherical | 0.98 | 1.00 | -68.00 | Escherichia coli XL1Blue | Escherichia sp. | - | 3.70 | https://doi.org/10.3762/bjnano.7.40 |
| 268 | Physical | 6.10 | Spherical | 0.98 | 1.00 | -68.00 | Bacillus subtilis 168 | Bacillus sp. | + | 1.50 | https://doi.org/10.3762/bjnano.7.40 |
| 269 | Green | 30.00 | Spherical | 0.20 | 1.00 | -29.20 | Pseudomonas aeruginosa PA01 | Pseudomonas sp. | - | 6.25 | https://doi.org/10.2147/IJN.S157958 |
| 270 | Green | 30.00 | Spherical | 0.20 | 1.00 | -29.20 | Escherichia coli UTI89 | Escherichia sp. | - | 12.50 | https://doi.org/10.2147/IJN.S157958 |
| 271 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Staphylococcus aureus | Staphylococcus sp. | + | 12.50 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 272 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Escherichia coli | Escherichia sp. | - | 3.13 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 273 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Enterococcus faecalis | Other | + | 3.13 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 274 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 3.13 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 275 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Bacillus subtilis | Bacillus sp. | + | 6.25 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 276 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 6.25 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 277 | Green | 14.00 | Spherical | 0.43 | 1.00 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 6.25 | https://doi.org/10.1016/j.micres.2015.09.009 |
| 278 | Green | 17.47 | Spherical | 0.34 | 1.00 | NAN | Streptococcus mutans | Streptococcus sp. | + | 1200.00 | https://doi.org/10.2147/IJN.S289243 |
| 279 | Green | 17.47 | Spherical | 0.34 | 1.00 | NAN | Methicillin-resistant Staphylococcus aureus | MRSA | + | 900.00 | https://doi.org/10.2147/IJN.S289243 |
| 280 | Green | 17.47 | Spherical | 0.34 | 1.00 | NAN | Escherichia coli ATCC 25922 | Escherichia sp. | - | 900.00 | https://doi.org/10.2147/IJN.S289243 |
| 281 | Green | 17.47 | Spherical | 0.34 | 1.00 | NAN | Salmonella typhimurium ATCC 14028 | Other | - | 900.00 | https://doi.org/10.2147/IJN.S289243 |
| 282 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Staphylococcus aureus ATCC 29213 | Staphylococcus sp. | + | 0.11 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 283 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Enterococcus faecalis ATCC 29212 | Other | + | 0.11 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 284 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Pseudomonas aeruginosa ATCC 27853 | Pseudomonas sp. | - | 0.11 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 285 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Salmonella typhimurium ATCC 23564 | Other | - | 0.11 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 286 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Escherichia coli ATCC 25922 | Escherichia sp. | - | 0.11 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 287 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Klebsiella pneumoniae ATCC 700603 | Klebsiella sp. | - | 7.10 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 288 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Shigella flexneri | Other | - | 0.89 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 289 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Staphylococcus aureus multiresistant | Staphylococcus sp. | + | 7.10 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 290 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Enterococcus faecalis multiresistant | Other | + | 1.70 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 291 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Pseudomonas aeruginosa multiresistant | Pseudomonas sp. | - | 1.70 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 292 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Shigella sonnei | Other | - | 0.89 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 293 | Green | 35.00 | Spherical | 0.17 | 1.00 | -19.60 | Escherichia coli multiresistant | Escherichia sp. | - | 0.89 | https://doi.org/10.1016/j.bioorg.2019.103425 |
| 294 | Chemical | 45.00 | Spherical | 0.13 | 1.00 | -28.80 | Staphylococcus aureus ATCC 25923 | Staphylococcus sp. | + | 190.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 295 | Chemical | 45.00 | Spherical | 0.13 | 1.00 | -28.80 | Bacillus subtilis AST5-2 | Bacillus sp. | + | 195.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 296 | Chemical | 45.00 | Spherical | 0.13 | 1.00 | -28.80 | Pseudomonas aeruginosa AL2-14B | Pseudomonas sp. | - | 188.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 297 | Chemical | 45.00 | Spherical | 0.13 | 1.00 | -28.80 | Klebsiella pneumoniae AWD5 | Klebsiella sp. | - | 184.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 298 | Chemical | 45.00 | Spherical | 0.13 | 1.00 | -28.80 | Escherichia coli ATCC 25922 | Escherichia sp. | - | 190.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 299 | Chemical | 20.00 | Rod | 0.22 | 0.71 | -23.50 | Staphylococcus aureus ATCC 25923 | Staphylococcus sp. | + | 358.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 300 | Chemical | 20.00 | Rod | 0.22 | 0.71 | -23.50 | Bacillus subtilis AST5-2 | Bacillus sp. | + | 350.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 301 | Chemical | 20.00 | Rod | 0.22 | 0.71 | -23.50 | Pseudomonas aeruginosa AL2-14B | Pseudomonas sp. | - | 348.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 302 | Chemical | 20.00 | Rod | 0.22 | 0.71 | -23.50 | Klebsiella pneumoniae AWD5 | Klebsiella sp. | - | 320.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 303 | Chemical | 20.00 | Rod | 0.22 | 0.71 | -23.50 | Escherichia coli ATCC 25922 | Escherichia sp. | - | 340.00 | https://doi.org/10.1038/s41598-017-18590-6 |
| 304 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Escherichia coli | Escherichia sp. | - | 2.00 | https://doi.org/10.1007/s12010-014-0934-y |
| 305 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Shigella sonnei | Other | - | 3.00 | https://doi.org/10.1007/s12010-014-0934-y |
| 306 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Klebsiella pneumoniae | Klebsiella sp. | - | 4.00 | https://doi.org/10.1007/s12010-014-0934-y |
| 307 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Pseudomonas aeruginosa | Pseudomonas sp. | - | 4.00 | https://doi.org/10.1007/s12010-014-0934-y |
| 308 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Bacillus subtilis | Bacillus sp. | + | 5.00 | https://doi.org/10.1007/s12010-014-0934-y |
| 309 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Staphylococcus aureus | Staphylococcus sp. | + | 5.50 | https://doi.org/10.1007/s12010-014-0934-y |
| 310 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Tannerella forsythia | Other | - | 5.50 | https://doi.org/10.1007/s12010-014-0934-y |
| 311 | Physical | 18.00 | Spherical | 0.33 | 1.00 | NAN | Vancomycin-resistant Enterococcus | Other | + | 6.00 | https://doi.org/10.1007/s12010-014-0934-y |